Copyright 2014 by The American Institute of Architects (AIA)

Exclusively published and distributed by AVITRU, LLC for the AIA

This Product MasterSpec Section is licensed by AVITRU, LLC to ClarkDietrich Building Systems ("Licensee").

This Product MasterSpec Section modifies the original MasterSpec text and does not include the full content of the original MasterSpec Section.

Revisions made to the original MasterSpec text are made solely by the Licensee and are not endorsed by, or representative of the opinions of, Avitru or The American Institute of Architects (AIA). Neither AIA nor Avitru are liable in any way for such revisions or for the use of this Product MasterSpec Section by any end user. A qualified design professional should review and edit the document to suit project requirements.

For more information, contact ClarkDietrich Building Systems, 9050 Centre Pointe Dr., Suite 400, West Chester, OH 45069; Phone: (513) 870-1100; Fax: (513) 870-1300; Website: www.clarkdietrich.com; Email: info@clarkdietrich.com.

For information about MasterSpec, contact Avitru at (800) 424-5080 or visit avitru.com.

SECTION 092400 - CEMENT PLASTERING

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Access Product MasterSpec Sections:

<Double click here to view the list of manufacturer Sections available at www.productmasterspec.com.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

SUMMARY

Section Includes:

Exterior vertical plasterwork (stucco).

Exterior horizontal and nonvertical plasterwork (stucco).

Interior vertical plasterwork.

Interior horizontal and nonvertical plasterwork.

PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

If needed, insert list of conference participants not mentioned in Section 013100 "Project Management and Coordination."

ACTION SUBMITTALS

Product Data: For each type of product.

Sustainable Design Submittals:

          - LEED v4 Submittals:

MR Credit: Building Product Disclosure and Optimization - Environmental Product Declarations (EPDs): Provide Type III EPDs from manufacturers that have third-party-verified environmental impact data. Excludes products fabricated from rigid PVC or CPVC plastic.

MR Credit: Building Product Disclosure and Optimization - Sourcing of Raw Materials: Provide recycled content of products showing percentage of postconsumer and/or preconsumer recycled content by weight and its associated cost. Excludes products fabricated from rigid PVC or CPVC plastic.

MR Credit: Building Product Disclosure and Optimization - Material Ingredients: Provide Health Product Declarations (HPD) from manufacturers with full disclosure of known hazards in compliance with the HPD Open Standard. Excludes products fabricated from rigid PVC or CPVC plastic.

MR Credit: Construction and Demolition Waste Management: Include a statement indicating percentage of materials diverted from disposal in landfills and incinerators, and where recyclable resources are directed back to the manufacturing process.

Retain "Shop Drawings" Paragraph below if Drawings do not show locations and details of control and expansion joints

Shop Drawings: Show locations and installation of control and expansion joints, including plans, elevations, sections, details of components, and attachments to other work.

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples.

Samples: For each type of factory-prepared finish coat and for each color and texture specified.

Samples for Initial Selection: For each type of factory-prepared finish coat and for each color and texture specified.

Samples for Verification: For each type of factory-prepared finish coat and for each color and texture specified, 12 by 12 inches (305 by 305 mm), and prepared on rigid backing.

QUALITY ASSURANCE

Mockups: Build mockups to verify selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for materials and execution.

If plaster has integral color or a special mockup requirement, revise first subparagraph below.

Build mockups for each substrate and finish texture indicated for cement plastering, including accessories.

Size: [100 sq. ft. (9 sq. m)] <Insert dimension> in surface area.

For interior plasterwork, simulate finished lighting conditions for review of mockups.

Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

DELIVERY, STORAGE, AND HANDLING

Store materials inside under cover, and keep them dry and protected against damage from weather, moisture, direct sunlight, surface contamination, corrosion, construction traffic, and other causes.

Protect cold-formed metal framing from corrosion, deformation, and other damage during delivery, storage, and handling as required by AISI's "Code of Standard Practice."

FIELD CONDITIONS

Comply with ASTM C926 requirements.

Exterior Plasterwork:

Apply and cure plaster to prevent plaster drying out during curing period. Use procedures required by climatic conditions, including moist curing, providing coverings, and providing barriers to deflect sunlight and wind.

Apply plaster when ambient temperature is greater than 40 deg F (4.4 deg C) and rising.

Protect plaster coats from freezing for not less than 48 hours after set of plaster coat has occurred.

Interior Plasterwork: Maintain room temperatures at greater than 40 deg F (4.4 deg C) for at least 48 hours before plaster application, and continuously during and after application.

Avoid conditions that result in plaster drying out during curing period. Distribute heat evenly; prevent concentrated or uneven heat on plaster.

Ventilate building spaces as required to remove water in excess of that required for hydrating plaster in a manner that prevents drafts of air from contacting surfaces during plaster application and until plaster is dry.

Factory-Prepared Finishes: Comply with manufacturer's written recommendations for environmental conditions for applying finishes.

PRODUCTS

Manufacturers and products listed in SpecAgent and MasterWorks Paragraph Builder are neither recommended nor endorsed by the AIA or Avitru. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

PERFORMANCE REQUIREMENTS

Retain "Fire-Resistance Ratings" Paragraph below if cement plastering is part of a fire-resistance-rated assembly. Indicate rating, testing agency, and testing agency's design designations on Drawings. Revise paragraph if fire-resistance rating is determined by prescriptive assemblies or calculation methods allowed by applicable codes.

Fire-Resistance Ratings: Where indicated, provide cement plaster assemblies identical to those of assemblies tested for fire resistance according to ASTM E119, and displaying a classification label from a qualified independent testing agency acceptable to authorities having jurisdiction.

Construct fire-resistance-rated partitions in compliance with tested assembly requirements[ indicated on Drawings].

Rated assemblies to be substantiated from applicable testing using proposed products, by Contractor.

METAL LATH

Coordinate lath selections with framing-spacing requirements detailed on Drawings and installation requirements. See "Metal Laths" Article in the Evaluations.

Expanded-Metal Lath: ASTM C847, cold-rolled carbon-steel sheet with ASTM A653/A653M, G60 (Z180), hot-dip galvanized-zinc coating.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide ClarkDietrich Building Systems; Diamond Mesh Lath or a comparable product by one of the following:

Alabama Metal Industries Company; a Gibraltar Industries company.

Phillips Manufacturing Co.

<Insert manufacturer's name>.

Retain "Recycled Content" Subparagraph below to specify recycled content if required. An alternative method of requiring recycled content is to retain requirement in Project's Division 01 sustainable design requirements Section that gives Contractor the option and responsibility to determine how recycled content requirements will be met.

Recycled Content: Postconsumer recycled content plus one-half of preconsumer recycled content not less than [25] <Insert number> percent.

Diamond-Mesh Lath: [Flat] [Self-furring], [2.5 lb/sq. yd. (1.4 kg/sq. m)] [3.4 lb/sq. yd. (1.8 kg/sq. m)].

Flat-rib lath is more rigid than diamond lath; it is unsuitable for contour lathing.

Flat-Rib Lath: Rib depth of not more than 1/8 inch (3.1 mm), [2.75 lb/sq. yd. (1.5 kg/sq. m)] [3.4 lb/sq. yd. (1.8 kg/sq. m)].

3/8-inch (10-mm) rib lath is often used where its rigidity is necessary for long spans.

Rib Lath: 3/8-inch (9.5-mm) Rib Lath: [3.4 lb/sq. yd. (1.8 kg/sq. m)] [4 lb/sq. yd. (2.2 kg/sq. m)].

Welded Wire Lath: ASTM C933, Class 1 galvanized coating complying with ASTM A641.

Retain "Basis-of-Design Product" Paragraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Structa Wire Corp. by ClarkDietrich Building Systems; [Structalath III] [Structalath Twin Trac] [Structa Mega Lath] [V Truss Corner] [V Truss Wall & Ceiling - Rib Lath] or comparable product by one of the following:

<Insert manufacturer's name>.

Welded Wire Lath:

Retain first option in "Weight" Subparagraph below for ClarkDietrich's "Structalath III"; second for "Structalath Twin Trac"; third for "Structa Mega Lath"; and fourth for "V Truss Wall & Ceiling - Rib Lath."

Weight: [1.0 lb/sq. yd. (0.5kg/sq. m)] [1.14 lb/sq. yd. (0.62 kg/sq. m)] [1.95 lb/sq. yd. (1.1 kg/sq. m)] [2.2 lb/sq. yd. (1.2 kg/sq. m)].

Retain "Exterior Corner Reinforcement - Profile" Subparagraph below for ClarkDietrich's "V Truss Corner."

Exterior Corner Reinforcement - Profile: [Straight] [Bullnose] [Arch] [One coat].

Wire-Fabric Lath:

Retain "Manufacturers" Subparagraph below and list of manufacturers to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Davis Wire; a Heico Wire Group company.

Jaenson Wire Company.

Keystone Steel & Wire Co.

K-Lath; a Tree Island Steel Ltd. company.

<Insert manufacturer's name>.

Welded-Wire Lath: ASTM C933; self-furring, [1.4 lb/sq. yd. (0.8 kg/sq. m)] [1.95 lb/sq. yd. (1.1 kg/sq. m)].

Woven-Wire Lath: ASTM C1032; self-furring, with stiffener wire backing, [1.1 lb/sq. yd. (0.6 kg/sq. m)] [1.4 lb/sq. yd. (0.8 kg/sq. m)].

Retain "Paper Backing" Paragraph below if required for expanded-metal and wire-fabric laths above. Verify paper backing is available with manufacturers.

Paper Backing: FS UU-B-790a, Type I, [Grade D, Style 2 vapor-permeable paper] [Grade B, Style 1a vapor-retardant paper] <Insert requirements>.

Provide paper-backed lath [unless otherwise indicated] [at exterior locations] [in locations indicated on Drawings] <Insert locations>.

ACCESSORIES

General: Comply with ASTM C1063, and coordinate depth of trim and accessories with thicknesses and number of plaster coats required.

If retaining requirements for trims, such as cornerbeads and casing beads that are fabricated from more than one material, indicate locations of each on Drawings.

Metal Accessories:

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

          - Basis-of-Design Product: Subject to compliance with requirements, provide products by ClarkDietrich Building Systems or comparable products by one of the following:

Alabama Metal Industries Company; a Gibraltar Industries company.

Phillips Manufacturing Co.

<Insert manufacturer's name>.

Retain "Foundation Weep Screed" Subparagraph below for exterior plaster to provide a means of removing water that penetrates wall cavities.

Foundation Weep Screed: Fabricated from hot-dip galvanized-steel sheet, ASTM A653/A653M, G60 (Z180) zinc coating.

Retain "Cornerite" Subparagraph below for reinforcing plaster at internal angles of plaster on solid bases and for restrained construction using expanded-metal lath (that is not otherwise lapped); see "Accessories" Article in the Evaluations.

Cornerite: Fabricated from expanded metal lath with ASTM A653/A653M, G60 (Z180), hot-dip galvanized-zinc coating.

Strip Lath: Fabricated from expanded-metal lath with ASTM A653/A653M, G60 (Z180), hot-dip galvanized zinc coating.

Retain "External- (Outside-) Corner Reinforcement" Subparagraph below for external (outside) corners of exterior plaster where cornerbeads are not used.

External- (Outside-) Corner Reinforcement: Fabricated from metal lath with ASTM A653/A653M, G60 (Z180), hot-dip galvanized-zinc coating.

Delete "Cornerbeads," "Casing Beads," "Control Joints," "Expansion Joints," and "Two-Piece Expansion Joints" subparagraphs below if only plastic trim is required.

Cornerbeads: Fabricated from [zinc] [or] [zinc-coated (galvanized) steel].

Retain applicable descriptions of cornerbeads in first four subparagraphs below. If more than one type is required and locations do not fit descriptions below, indicate locations on Drawings or by inserting requirements.

Smallnose cornerbead with expanded flanges; use unless otherwise indicated.

Basis-of-Design Product: Subject to compliance with requirements, provide ClarkDietrich Building Systems; #1A Expanded Corner Bead or comparable product.

Smallnose cornerbead with perforated flanges; use on curved corners.

Smallnose cornerbead with expanded flanges reinforced by perforated stiffening rib; use on columns and for finishing unit masonry corners.

Basis-of-Design Product: Subject to compliance with requirements, provide ClarkDietrich Building Systems; #2A Expanded Corner Bead or comparable product.

Bullnose cornerbead, radius 3/4 inch (19.1 mm) minimum, with expanded flanges; use at locations indicated on Drawings.

Casing Beads: Fabricated from [zinc] [or] [zinc-coated (galvanized) steel]; square-edged style; with expanded flanges.

Basis-of-Design Product: Subject to compliance with requirements, provide ClarkDietrich Building Systems; #66X Expanded Flange Casing Bead or comparable product.

Control Joints: Fabricated from [zinc] [or] [zinc-coated (galvanized) steel]; one-piece-type, folded pair of unperforated screeds in M-shaped configuration; with perforated flanges and removable protective tape on plaster face of control joint.

Basis-of-Design Product: Subject to compliance with requirements, provide ClarkDietrich Building Systems; Zinc Control Joint or comparable product.

Expansion Joints: Fabricated from [zinc] [or] [zinc-coated (galvanized) steel]; folded pair of unperforated screeds in M-shaped configuration; with expanded flanges.

Basis-of-Design Product: Subject to compliance with requirements, provide ClarkDietrich Building Systems; #15 Double-V Control Joint or comparable product.

Two-Piece Expansion Joints: Fabricated from [zinc] [or] [zinc-coated (galvanized) steel]; formed to produce slip-joint and square-edged reveal that is adjustable from 1/4 to 5/8 inch (6 to 16 mm) wide; with perforated flanges.

Basis-of-Design Product: Subject to compliance with requirements, provide ClarkDietrich Building Systems; #40 Two-Piece Expansion Joint or comparable product.

Plastic Accessories: Manufactured from rigid PVC or CPVC plastic.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

          - Basis-of-Design Product: Subject to compliance with requirements, provide products by Vinyl Corp. or comparable product by one of the following:

Alabama Metal Industries Company; a Gibraltar Industries company.

Phillips Manufacturing Co.

<Insert manufacturer's name>.

Cornerbeads: With perforated flanges.

Retain applicable descriptions of cornerbeads in first two subparagraphs below. If more than one is required and locations do not fit descriptions below, indicate locations on Drawings or by inserting requirements.

Smallnose cornerbead is recommended by manufacturers for use where durable corner is required; use on columns and for finishing unit masonry corners.

Smallnose cornerbead; use unless otherwise indicated.

Subject to compliance with requirements, provide Vinyl Corp.; #1 Corner Bead or comparable product.

Bullnose cornerbead, radius 3/4 inch (19. mm) minimum; use at locations indicated on Drawings.

Subject to compliance with requirements, provide Vinyl Corp.; Bullnose Corner Bead or comparable product.

Casing Beads: With perforated flanges in depth required to suit plaster bases indicated and flange length required to suit applications indicated.

Square-edge style; use unless otherwise indicated.

              - Subject to compliance with requirements, provide Vinyl Corp.; Casing Bead or comparable product.

Bullnose style, radius 3/4 inch (19.1 mm) minimum; use at locations indicated on Drawings.

              - Subject to compliance with requirements, provide Vinyl Corp.; Bullnose Casing Bead or comparable product.

Control Joints: One-piece-type, folded pair of unperforated screeds in M-shaped configuration; with perforated flanges and removable protective tape on plaster face of control joint.

Subject to compliance with requirements, provide Vinyl Corp.; Control Joint or comparable product.

Expansion Joints: Two-piece type, formed to produce slip-joint and square-edged [1/2-inch- (13-mm-)] [1-inch- (25-mm-)] [1-1/2-inch- (38-mm-)] <Insert dimension> wide reveal; with perforated concealed flanges.

            - Subject to compliance with requirements, provide Vinyl Corp.; Expansion Joint or comparable product.

          - Soffit Reveals: PVC reveals complying with ASTM C1047.

            - Subject to compliance with requirements, provide Vinyl Corp.; Channel Reveal or comparable product.

Soffit Vents:

            - Subject to compliance with requirements, provide Vinyl Corp.; Soffit Vent or comparable product.

MISCELLANEOUS MATERIALS

Water containing salt, alum, or plaster residue accelerates plaster set and may cause efflorescence. Water containing organic or vegetable matter may retard plaster set, cause staining, and interfere with plaster bond.

Water for Mixing and Finishing Plaster: Potable and free of substances capable of affecting plaster set or of damaging plaster, lath, or accessories.

Retain "Fiber for Base Coat" Paragraph below if required. Fibers can be added to plaster base-coat mixes to increase cohesiveness, tensile strength, and impact resistance and to reduce shrinkage.

Fiber for Base Coat: Alkaline-resistant glass or polypropylene fibers, 1/2 inch (13 mm) long, free of contaminants, manufactured for use in cement plaster.

Retain "Bonding Compound" Paragraph below where plaster is adhered to structurally sound unit masonry or monolithic concrete.

Bonding Compound: ASTM C932.

Fasteners for Attaching Metal Lath to Substrates: ASTM C1063.

Generally, retain "Wire" Paragraph below. Wire, in various diameters, is used for tying metal lath to framing and supports.

Wire: ASTM A641/A641M, Class 1 zinc coating, soft temper, not less than 0.0475-inch (1.21-mm) diameter unless otherwise indicated.

Sound-Attenuation Blankets: ASTM C665, Type I (blankets without membrane facing) produced by combining thermosetting resins with mineral fibers manufactured from glass, slag wool, or rock wool.

Fire-Resistance-Rated Assemblies: Comply with mineral-fiber requirements of assembly.

Retain "Recycled Content" Subparagraph below to specify recycled content if required. An alternative method of requiring recycled content is to retain requirement in Project's Division 01 sustainable design requirements Section that gives Contractor the option and responsibility to determine how recycled content requirements will be met.

Recycled Content: Postconsumer recycled content plus one-half of preconsumer recycled content not less than <Insert number> percent.

PLASTER MATERIALS

Retain second option in "Portland Cement" Paragraph below if sulfate resistance is required.

Portland Cement: ASTM C150/C150M, [Type I] [Type II].

Color for Finish Coats: [White] [Gray].

Masonry Cement: ASTM C91, Type N.

Color for Finish Coats: [White] [Gray].

Retain "Plastic Cement" Paragraph below only after verifying availability in Project area.

Plastic Cement: ASTM C1328.

If applicable, insert requirements for blended hydraulic cements here.

Colorants for Job-Mixed Finish Coats: Colorfast mineral pigments that produce finish plaster color [to match Architect's sample] <Insert requirements>.

Lime: ASTM C206, Type S; or ASTM C207, Type S.

Sand Aggregate: ASTM C897.

Color for Job-Mixed Finish Coats: [White] [In color matching Architect's sample].

Retain "Perlite Aggregate" Paragraph below if fire-resistance-rated cement plaster assemblies require lightweight perlite aggregate rather than sand.

Perlite Aggregate: ASTM C35.

Exposed aggregates, such as washed gravel, granite, and colored glass, can be used in finish coats; large stones can also be hand placed in finish coats. Option in "Exposed Aggregates for Finish Coats" Paragraph below is an example only.

Exposed Aggregates for Finish Coats: [For marblecrete finish, clean, sound, crushed marble matching color and size gradation of Architect's sample] <Insert requirements>.

If polymer additives or air-entraining agents are required or allowed, insert requirements here.

Coordinate ready-mixed finish-coat plaster with base-coat requirements to ensure compatibility.

Ready-Mixed Finish-Coat Plaster: Mill-mixed portland cement, aggregates, coloring agents, and proprietary ingredients.

Retain "Manufacturers" Subparagraph below and list of manufacturers to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

California Stucco Products Corp.

El Rey Stucco Solutions; Parex USA.

Florida Stucco.

LaHabra Stucco Solutions; Parex USA.

Omega Products International, Inc.

QUIKRETE.

Shamrock Stucco LLC.

SonoWall, BASF Corp.

<Insert manufacturer's name>.

Color: [Match Architect's sample] [As selected by Architect from manufacturer's full range] <Insert color>.

Coordinate acrylic-based coatings with base-coat requirements to ensure compatibility.

Acrylic-Based Finish Coatings: Factory-mixed acrylic-emulsion coating systems formulated with colorfast mineral pigments and fine aggregates; for use over cement plaster base coats. Include manufacturer's recommended primers and sealing topcoats for acrylic-based finishes.

Retain "Manufacturers" Subparagraph below and list of manufacturers to require products from manufacturers listed or a comparable product from other manufacturers.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

California Stucco Products Corp.

Dryvit Systems, Inc.

El Rey Stucco Solutions; Parex USA.

Finestone, BASF Corp.

Master Wall Inc.

Omega Products International, Inc.

Senergy, BASF Corp.

Shamrock Stucco LLC.

SonoWall, BASF Corp.

Sto Corp.

Stuc-O-Flex International, Inc.

<Insert manufacturer's name>.

Color: [Match Architect's sample] [As selected by Architect from manufacturer's full range] <Insert color>.

PLASTER MIXES

General: Comply with ASTM C926 for applications indicated.

Retain "Fiber Content" Subparagraph below for greater plaster strength and crack resistance.

Fiber Content: Add fiber to base-coat mixes after ingredients have mixed at least two minutes. Comply with fiber manufacturer's written instructions for fiber quantities in mixes, but do not exceed 1 lb of fiber/cu. yd. (0.6 kg of fiber/cu. m) of cementitious materials.

If retaining perlite aggregate for fire-resistance-rated assemblies, insert mix requirements for perlite-aggregate plaster.

Retain applicable base coats in "Base-Coat for Use over Metal Lath" Paragraph below, or insert others to suit Project. Coordinate with requirements retained in "Plaster Materials" Article.

Base-Coat Mixes for Use over Metal Lath: Scratch and brown coats for three-coat plasterwork as follows:

Portland Cement Mixes:

Decreasing the proportion of lime in the cementitious-material mix produces a harder surface but increases the possibility of cracking.

Scratch Coat: For cementitious material, mix 1 part portland cement and [0 to 3/4] [3/4 to 1-1/2] parts lime. Use 2-1/2 to 4 parts aggregate per part of cementitious material.

Brown Coat: For cementitious material, mix 1 part portland cement and [0 to 3/4] [3/4 to 1-1/2] parts lime. Use 3 to 5 parts aggregate per part of cementitious material, but not less than volume of aggregate used in scratch coat.

Masonry Cement Mixes:

Scratch Coat: Mix 1 part masonry cement and 2-1/2 to 4 parts aggregate.

Brown Coat: Mix 1 part masonry cement and 3 to 5 parts aggregate, but not less than volume of aggregate used in scratch coat.

Portland and Masonry Cement Mixes:

Scratch Coat: For cementitious material, mix 1 part portland cement and 1 part masonry cement. Use 2-1/2 to 4 parts aggregate per part of cementitious material.

Brown Coat: For cementitious material, mix 1 part portland cement and 1 part masonry cement. Use 3 to 5 parts aggregate per part of cementitious material, but not less than volume of aggregate used in scratch coat.

Plastic Cement Mixes:

Scratch Coat: Mix 1 part plastic cement and 2-1/2 to 4 parts aggregate.

Brown Coat: Mix 1 part plastic cement and 3 to 5 parts aggregate, but not less than volume of aggregate used in scratch coat.

Portland and Plastic Cement Mixes:

Scratch Coat: For cementitious material, mix 1 part plastic cement and 1 part portland cement. Use 2-1/2 to 4 parts aggregate per part of cementitious material.

Brown Coat: For cementitious material, mix 1 part plastic cement and 1 part portland cement. Use 3 to 5 parts aggregate per part of cementitious material, but not less than volume of aggregate used in scratch coat.

Based on the absorption characteristics of plaster substrates, retain applicable "Base-Coat Mixes for Use over (Unit Masonry) (and) (Concrete)" paragraphs below for two-coat plasterwork, or insert requirements to suit Project. First paragraph below is for "low-absorption" plaster bases, second is for "high-absorption" plaster bases. If retaining both paragraphs, revise to ensure that locations of mixes are clearly identified.

Base-Coat Mixes for Use over [Unit Masonry] [and] [Concrete]: Single base (scratch) coat for two-coat plasterwork on low-absorption plaster bases as follows:

According to ASTM C926, mixes in "Portland Cement Mix," "Portland and Masonry Cement Mix," and "Plastic Cement Mix" subparagraphs below are suitable for use over "low-absorption" plaster bases, such as brick, concrete, and dense, smooth clay tile. Coordinate with requirements retained in "Plaster Materials" Article.

Portland Cement Mix: For cementitious material, mix 1 part portland cement and 0 to 3/4 part lime. Use 2-1/2 to 4 parts aggregate per part of cementitious material.

Portland and Masonry Cement Mix: For cementitious material, mix 1 part portland cement and 1 part masonry cement. Use 2-1/2 to 4 parts aggregate per part of cementitious material.

Plastic Cement Mix: Use 1 part plastic cement and 2-1/2 to 4 parts aggregate.

Base-Coat Mixes for Use over [Unit Masonry] [and] [Concrete]: Single base (scratch) coat for two-coat plasterwork on high-absorption plaster bases as follows:

According to ASTM C926, mixes in "Portland Cement Mix," "Masonry Cement Mix," "Portland and Masonry Cement Mix," and "Plastic Cement Mix" subparagraphs below are suitable for use over "high-absorption" plaster bases, such as concrete unit masonry, absorptive brick, and tile. Coordinate with requirements retained in "Plaster Materials" Article.

Portland Cement Mix: For cementitious material, mix 1 part portland cement and 3/4 to 1-1/2 parts lime. Use 2-1/2 to 4 parts aggregate per part of cementitious material.

Masonry Cement Mix: Use 1 part masonry cement and 2-1/2 to 4 parts aggregate.

Portland and Masonry Cement Mix: For cementitious material, mix 1 part portland cement and 1 part masonry cement. Use 2-1/2 to 4 parts aggregate per part of cementitious material.

Plastic Cement Mix: Use 1 part plastic cement and 2-1/2 to 4 parts aggregate.

Retain applicable finish coats in "Job-Mixed Finish-Coat Mixes" and "Factory-Prepared Finish-Coat Mixes" paragraphs below, or insert others to suit Project. Coordinate with requirements retained in "Plaster Materials" Article and with requirements for base coats.

Job-Mixed Finish-Coat Mixes:

Decreasing the proportion of lime in the mix produces a harder surface but increases the possibility of cracking.

Portland Cement Mix: For cementitious materials, mix 1 part portland cement and [3/4 to 1-1/2] [1-1/2 to 2] parts lime. Use 1-1/2 to 3 parts aggregate per part of cementitious material.

Masonry Cement Mix: Use 1 part masonry cement and 1-1/2 to 3 parts aggregate.

Portland and Masonry Cement Mix: For cementitious materials, mix 1 part portland cement and 1 part masonry cement. Use 1-1/2 to 3 parts aggregate per part of cementitious material.

Plastic Cement Mix: Use 1 part plastic cement and 1-1/2 to 3 parts aggregate.

Factory-Prepared Finish-Coat Mixes: For [ready-mixed finish-coat plasters] [acrylic-based finish coatings], comply with manufacturer's written instructions.

EXECUTION

EXAMINATION

Examine substrates and conditions, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance of the Work.

Proceed with installation only after unsatisfactory conditions have been corrected.

PREPARATION

Protect adjacent work from soiling, spattering, moisture deterioration, and other harmful effects caused by plastering.

Prepare smooth, solid substrates for plaster according to ASTM C926.

INSTALLATION, GENERAL

Revise "Fire-Resistance-Rated Assemblies" Paragraph below if fire-resistance rating is determined by prescriptive assemblies or calculation methods allowed by applicable codes.

Fire-Resistance-Rated Assemblies: Install components according to requirements for design designations from listing organization and publication indicated on Drawings.

Show locations of sound-attenuation blankets on Drawings, or revise "Sound-Attenuation Blankets" Paragraph below to suit Project.

Sound-Attenuation Blankets: Where required, install blankets before installing lath unless blankets are readily installed after lath has been installed on one side.

INSTALLING METAL LATH

Metal Lath: Install according to ASTM C1063.

Retain appropriate lath for each location specified in "Partition Framing and Vertical Furring," "Flat-Ceiling and Horizontal Framing," "Curved-Ceiling Framing," and "On Solid Surfaces, Not Otherwise Furred" subparagraphs below, or delete subparagraphs if only one type of lath is required or if locations of each type of lath are shown on Drawings. See "Metal Laths" Article in the Evaluations.

Partition Framing and Vertical Furring: Install [flat-diamond-mesh] [flat-rib] [welded-wire] [woven-wire] lath.

Diamond-mesh lath requires closely spaced supports when used on ceilings.

Flat-Ceiling and Horizontal Framing: Install [flat-diamond-mesh] [flat-rib] [3/8-inch (10-mm) rib] [welded-wire] [woven-wire] lath.

Curved-Ceiling Framing: Install [flat-diamond-mesh] [welded-wire] [flat-woven-wire] lath.

On Solid Surfaces, Not Otherwise Furred: Install self-furring, [diamond-mesh] [welded-wire] [woven-wire] lath.

INSTALLING WIRE LATH

Retain one of two "Installation" Paragraphs below to suit project. Retain first for ClarkDietrich's "Structalath III," "Structalath Twin Trac," and "Structa Mega Lath"; and second for "V Truss Wall & Ceiling - Rib Lath."

See manufacturer's written instructions posted at www.structawire.com.

Installation: In accordance with IAPMO UES ER 2017; fastener type and spacing in accordance with ASTM C1063 with the exception that fasteners may attach lath to framing supports at [furring crimps on the vertical cross wire] [intersection of the longitudinal wire and cross wire] [any point along longitudinal wire]. [Nail] [Screw] [Staple] lath fastening points to coincide with longitudinal wires.

Retain first "Maximum Support Spacing" Subparagraph below for ClarkDietrich's "Structalath III"; second for "Structalath Twin Trac"; and third for "Structa Mega Lath."

Maximum Support Spacing: 16 inch (406 mm) o.c.

Retain one of two options in "Maximum Support Spacing" Subparagraph below; see manufacturer's written instructions for ClarkDietrich's "Structalath Twin Trac," posted at www.structawire.com.

Maximum Support Spacing: In accordance with Table 3 of ASTM C1063 as an alternative to [1.14-lb/sq. yd. (0.62-kg/sq. m) welded wire] [2.5-lb/sq. yd. (1.4-kg/sq. m) diamond-mesh metal lath].

Retain one of two options in "Maximum Support Spacing" Subparagraph below; see manufacturer's written instructions for ClarkDietrich's "Structa Mega Lath," posted at www.structawire.com.

Maximum Support Spacing: In accordance with Table 3 of ASTM C1063 as an alternative to [1.14-lb/sq. yd. (0.62-kg/sq. m) woven wire] [3.4-lb/sq. yd. (1.8-kg/sq. m) diamond-mesh metal lath]. Lath is approved for 24 inches (610 mm) o.c. and lapped one mesh.

Installation: In accordance with IAPMO UES ER 2017; fastener type and attachment in accordance with ASTM C1063 with exception that fasteners attach lath at framing supports every second rib, either at furring crimps on vertical cross wire, at intersection of longitudinal wire and cross wire, or any point along longitudinal wire welded to furring crimp. When using screws, deformation of rib is preferable.

Retain one of two options in "Maximum Support Spacing" Subparagraph below; see manufacturer's written instructions for ClarkDietrich's "V Truss Wall & Ceiling - Rib Lath," posted at www.structawire.com.

Maximum Support Spacing: [1.4-lb/sq. yd. (0.75-kg/sq. m) woven wire] [3.4-lb/sq. yd. (1.8-kg/sq. m) diamond mesh metal lath] in accordance with Table 3 of ASTM C1063. Lap lath minimum one mesh at sides. Lap end laps a minimum one mesh over supports. Stagger ends of sheets between courses.

INSTALLING ACCESSORIES

Install according to ASTM C1063 and ASTM C1047 at locations indicated on Drawings.

Reinforcement for External (Outside) Corners:

Install [lath-type, external-corner reinforcement] [cornerbead] at exterior locations.

Install cornerbead at interior locations.

Retain "Control Joints" Paragraph below if control-joint locations are not detailed on Drawings.

Control Joints: Locate as approved by Architect for visual effect and as follows:

As required to delineate plasterwork into areas (panels) of the following maximum sizes:

Vertical Surfaces: 144 sq. ft. (13.4 sq. m).

Horizontal and Other Nonvertical Surfaces: 100 sq. ft. (9.3 sq. m).

At distances between control joints of not greater than 18 feet (5.5 m) o.c.

As required to delineate plasterwork into areas (panels) with length-to-width ratios of not greater than 2-1/2:1.

Where control joints occur in surface of construction directly behind plaster.

Where plasterwork areas change dimensions, to delineate rectangular-shaped areas (panels) and to relieve the stress that occurs at the corner formed by the dimension change.

PLASTER APPLICATION

General: Comply with ASTM C926.

Do not deviate more than plus or minus 1/4 inch in 10 feet (6 mm in 3 m) from a true plane in finished plaster surfaces when measured by a 10-foot (3-m) straightedge placed on surface.

Finish plaster flush with metal frames and other built-in metal items or accessories that act as a plaster ground unless otherwise indicated. Where casing bead does not terminate plaster at metal frame, cut base coat free from metal frame before plaster sets and groove finish coat at junctures with metal.

Retain subparagraph below if plaster surfaces are to receive field-applied finishes.

Provide plaster surfaces that are ready to receive field-applied finishes indicated.

Bonding Compound: Apply on [unit masonry] [and] [concrete] substrates for direct application of plaster.

Walls; Base-Coat Mixes for Use over Metal Lath: For scratch and brown coats, for three-coat plasterwork with 3/4-inch (19.1-mm) total thickness, as follows:

Retain one of five subparagraphs below or, if retaining more than one, indicate locations of each by inserts, on Drawings, or in schedules. Coordinate with requirements in "Plaster Mixes" Article.

Portland cement mixes.

Masonry cement mixes.

Portland and masonry cement mixes.

Plastic cement mixes.

Portland and plastic cement mixes.

Ceilings; Base-Coat Mixes for Use over Metal Lath: For scratch and brown coats, for three-coat plasterwork and having [1/2-inch (13-mm) total thickness] [3/4-inch (19.1-mm) total thickness for metal lath on concrete], as follows:

Retain one of five subparagraphs below or, if retaining more than one, indicate locations of each by inserts, on Drawings, or in schedules. Coordinate with requirements in "Plaster Mixes" Article.

Portland cement mixes.

Masonry cement mixes.

Portland and masonry cement mixes.

Plastic cement mixes.

Portland and plastic cement mixes.

Walls; Base-Coat Mix: For base (scratch) coat, for two-coat plasterwork and having [3/8-inch (10-mm) thickness on masonry] [1/4-inch (6-mm) thickness on concrete], as follows:

Retain one of five subparagraphs below or, if retaining more than one, indicate locations of each by inserts, on Drawings, or in schedules. Coordinate with requirements in "Plaster Mixes" Article.

Portland cement mix.

Masonry cement mix.

Portland and masonry cement mix.

Plastic cement mix.

Portland and plastic cement mix.

Ceilings; Base-Coat Mix: For base (scratch) coat, for two-coat plasterwork and having 1/4-inch (6-mm) thickness on concrete, as follows:

Retain one of five subparagraphs below or, if retaining more than one, indicate locations of each by inserts, on Drawings, or in schedules. Coordinate with requirements in "Plaster Mixes" Article.

Portland cement mix.

Masonry cement mix.

Portland and masonry cement mix.

Plastic cement mix.

Portland and plastic cement mix.

If various finishes are required, indicate locations of each on Drawings or by inserts in "Plaster Finish Coats" Paragraph below.

Plaster Finish Coats: Apply to provide [float] [dash] [scraped trowel-textured] [skip trowel-textured] [brocade (knock-down dash)] [trowel sweep] [combed] [sacked (California mission)] [English] [marblecrete] <Insert requirements> finish to match Architect's sample.

Acrylic-Based Finish Coatings: Apply coating system, including primers, finish coats, and sealing topcoats, according to manufacturer's written instructions.

Concealed Exterior Plasterwork: Where plaster application is used as a base for adhered finishes, omit finish coat.

Concealed Interior Plasterwork:

Where plaster application is concealed behind built-in cabinets, similar furnishings, and equipment, apply finish coat.

Where plaster application is concealed above suspended ceilings and in similar locations, omit finish coat.

Where tile or other finishes are adhered to plaster, verify that plasterwork specified complies with requirements for setting materials.

Where plaster application is used as a base for adhesive application of tile and similar finishes, omit finish coat.

PLASTER REPAIRS

Repair or replace work to eliminate cracks, dents, blisters, buckles, crazing and check cracking, dry outs, efflorescence, sweat outs, and similar defects and where bond to substrate has failed.

CLEANING AND PROTECTION

Remove temporary protection and enclosure of other work after plastering is complete. Promptly remove plaster from door frames, windows, and other surfaces not indicated to be plastered. Repair floors, walls, and other surfaces stained, marred, or otherwise damaged during plastering.

END OF SECTION 092400